## Slide 1: Explosion Welding
Keith Powell
Michael Fernandez
Staton Burrell

## Slide 2: Basics
Explosion welding is a solid-state process that produces a high velocity interaction of dissimilar metals by a controlled detonation
Oxides found on material surfaces must be removed by effacement or dispersion
Surface atoms of two joining metals must come into intimate contact to achieve metallic bond

## Slide 3: Advantages
No heat-affected zone (HAZ)
Only minor melting
Material melting temperatures and coefficients of thermal expansion differences do not affect the final product
The shock front compresses and heats the explosive material which exceeds the sonic velocity of undetonated explosives

## Slide 4: Component Terminology
Base component
  Joined to cladder
  Remains stationary
  Supported by anvil
Cladding metal
  Thin plate in direct contact with explosives
  Can be shielded by flyer plate

## Slide 5
Flyer plate
  Sacrificial plate placed between explosive material and cladder plate
  Used to protect cladder metal
Interlayer
  Thin metal layer
  Enhances joining of cladder to base plate
Anvil
  Surface of which the backer rests during explosion

## Slide 6
Standoff
  Distance between cladder and base plate before explosion
Bond Window
  A range of variable in process such as velocity, dynamic bend, and standoff distance that result in successful weld
Bonding Operation
  Detonation of explosives that result in a weld

## Slide 7: Principle of Explosion
Cladder metal can be placed parallel or inclined to the base plate
Explosive material is distributed over top of cladder metal
Upon detonation, cladder plate collides with base plate to form weld

## Slide 8: Placement of Cladder metal-parallel
Standoff distance predetermined and unique to material combination
  Achieved by placing shims between plates
  Shims designed to be consumed by explosion wave and do not affect weld
Usually ranges between 0.5-2 times the thickness of cladder plate
Cladder must reach critical velocity before impact

## Slide 9: Cladder placement-Angled
Where:
Vc = collision velocity
VD = detonation velocity
Vp = plate Collision velocity
α = preset angle
β = dynamic bend angle
γ = collision angle
Vc
VD
Vp

## Slide 10: Explosive material
High velocity (14750-25000 ft/s)
  Trinitrotoluene (TNT)
  Cyclotrimethylenetrinitramine (RDX)
  Pentaerythritol Tetranitrate (PETN)
Mid-low velocity (4900-47500 ft/s)
  Ammonium nitrate
  Ammonium perchlorate
  Amatol

## Slide 11: Assuring a good weld
Three types of detonation wave welds
  Shock wave develops if sonic velocity is greater than 120% of material sonic velocity (type 1)
  Detached shock wave results when detonation velocity is between 100% and 120% of material sonic velocity (type 2)
  No shock wave is produced if detonation velocity is less than material sonic velocity (type 3)

## Slide 12: Assuring a good weld
Type 1
  Material behind shock wave is compressed to peak pressure and density
  Creates significant plastic deformation locally and results in considerable ‘shock hardening’
Type 2 & 3
  Pressure is generated ahead of collision point of metals
  When subject to large pressures, metal ahead of collision point flows into spaces between plates and takes form of high-velocity jet
  Effaces material and removes unwanted oxides and other unwanted surface films
  No bulk diffusion and only localized melting

## Slide 13: Assuring a good weld
Detonation velocity is a function of
  Explosive type
  Composition of explosive
  Thickness of explosive layer
  Can be found in tables

## Slide 14: Assuring a good weld
Sonic velocity of cladding material can calculated using:
Where:
K = adiabatic bulk modulus
ρ = cladding material density
E = Young’s Modulus of cladding material
ע = Poisson’s ratio of cladding material

## Slide 15: Applications
Any metal with sufficient strength and ductility can be joined

## Slide 16: Applications
Can weld large areas of metal
Can weld inside and outside surfaces of pipes
Transition joints can be made

## Slide 17: History
Arnold Holtzman and a team at DuPont in Delaware put a lot of research into developing the process.
Holtzman filed for a US patent in 1962 for explosion welding, received the patent in 1964 and began commercial production of bi-metallic explosion welded clad in 1965.
Detaclad licensed the process and was bought by Dynamic Materials Corporation (DMC).
Other companies have merged with DMC and acquired the current name DMC Groupe SNPE making them a worldwide company.
Notes: US locations: colorado, pennsylvania, connecticut.
Europe locations: France, Germany, Sweden

## Slide 18: Common industries that use explosion welding
  Chemical Processing
Petroleum Refining
Hydrometallurgy
Aluminum Smelting
Shipbuilding
Electrochemical
Oil & Gas
Power Generation
Cryogenic Processing
Pulp & Paper
Air conditioning & Chillers
Metal Production

## Slide 19: Examples

## Slide 20: Examples
3” Diameter AI/SS Ring
Copper/Stainless 12” UHV Assembly

## Slide 21: Examples
United States dimes and quarters are presently a clad “sandwich” of copper inner-core and a silver-colored nickel-copper alloy

## Slide 22: Works Cited
http://www.annualreviews.org/doi/pdf/10.1146/annurev.ms.05.080175.001141
http://www.authorstream.com/Presentation/rock354-421051-explosive-welding-final-unconventional-machining-mp-iii-education-ppt-powerpoint/
Young, G (2004). "Explosion Welding, Technical Growth and Commercial History" (PDF). Dynamic Materials Corporation. http://www.dynamicmaterials.com/data/brochures/1-%20Young%20Paper%20on%20EXW%20History.pdf. Retrieved 2010-11-29